| A 1. | Identify types of laboratory testing performed at the facility being audited. | ___Sat ___Unsat ___N/A |
| --- | --- | --- |
|  | ___Chemical | ___Tensile | ___Charpy V Notch | ___Dynamic Tear |  |
|  | ___Weld ability | ___Wedge | ___Bend | ___Hardness |  |
|  | ___Other (specify): |  |
|  | b. Identify which test processes were witnessed and which were verified by objective quality evidence. |  |
| A 2. | Do the supplier's procedures contain requirements for method and location for obtaining test specimens and do these requirements meet applicable material specifications? | ___Sat ___Unsat ___N/A |
| A 3. | a. Do the supplier's procedures contain requirements identifying the specific number of test specimens required for each type of test? | ___Sat ___Unsat ___N/A |
|  | b. Do these meet applicable material specifications? | ___Sat ___Unsat ___N/A |
| A 4. | Review the method for identifying test specimens to heat, melt, lot, as applicable and the system for maintaining this identity through the laboratory process, including any machining of the specimen. | ___Sat ___Unsat ___N/A |
|  | b. Is the system adequate for maintaining test specimen identifies and trace ability? | ___Sat ___Unsat ___N/A |
| B 5. | Review a sample of completely machined test specimen’s specification (e.g. ASTM A-370 for ferrous material). Record number of samples reviewed. | ___Sat ___Unsat ___N/A |
| A 6. | Review the supplier's policy for retests as a result of test failure and assure that it meets applicable specification requirements. Explain, if unsatisfactory. | ___Sat ___Unsat ___N/A |
| A 7. | Is the testing performed to written procedure? | ___Sat ___Unsat ___N/A |
| B 8. | Is the applicable test procedure readily available to the Individual performing the test? | ___Sat ___Unsat ___N/A |
| A 9. | Does the procedure contain specific parameters and correct accept/reject criteria? | ___Sat ___Unsat ___N/A |
| B 10. | Is the test equipment being used in compliance with the specification/procedures? | ___Sat ___Unsat ___N/A |
| A 11. | Does the test equipment have objective quality evidence of being currently in calibration? | ___Sat ___Unsat ___N/A |
| A 12. | If applicable (charpy and dynamic tear), is the test specimen at the correct temperature at the time of the test? | ___Sat ___Unsat ___N/A |
| A 13. | Is the test specimen identified and traceable back to applicable heat and/or lot? | ___Sat ___Unsat ___N/A |
| B 14. | Review and identify a sample of test reports to ensure that data recorded satisfies specification requirement. | ___Sat ___Unsat ___N/A |

Additional Comments/Concerns: