NOTE - ALL QUESTIONS ON THIS AUDITOR'S PROCESS GUIDE ARE CONSIDERED 
PRIORITY CODE "A" EXCEPT QUESTION #24 WHICH IS CODED "B"

| 1. | a. Identify types of nondestructive testing performed at the facility being audited: |  |
| --- | --- | --- |
|  | ___MT | ___UT | ___PT | ___ET |  |
|  | ___RT | ___VT |  |  |  |
|  | ___Other (specify): |  |
|  | b. Identify which test processes were witnessed and which were verified by objective quality evidence. |  |
| 2. | Are applicable NDT procedures available and approved (IF REQUIRED)? Identify procedure number, revision, date and applicable Approval Number (if required). |  |
|  | MT Procedure ______________ | Rev. ___ | Date _______ | # _________ |  |
|  | PT Procedure _______________ | Rev. ___ | Date _______ | # _________ |  |
|  | UT Procedure _______________ | Rev. ___ | Date _______ | # _________ |  |
|  | VT Procedure _______________ | Rev. ___ | Date _______ | # _________ |  |
|  | ET Procedure _______________ | Rev. ___ | Date _______ | # _________ |  |
|  | RT Procedure _______________ | Rev. ___ | Date _______ | # _________ |  |
| Personnel Qualification: |
| 3. | Are all NDT personnel, including the examiner, recertified by examination at a minimum interval as required by specification? | ___ Yes ___No |
| 4. | Are adequate records available to administer personnel qualification; e.g. name, evidence of examination given, grade, re-certification dates, signature of examiner? | ___Sat ___Unsat |
| 5. | Do records include evidence of performance of applicable NDT during the last 6 months to maintain qualification? | ___Sat ___Unsat |
| 6. | a. Are vision test records available? | ___Sat ___Unsat |
|  | b. Do these records indicate a J1 Jaeger test or equivalent and brightness discrimination, on an annual basis? | ___Sat ___Unsat |
| 7. | Do vision test records note corrective aids (glasses) when applicable? | ___Sat ___Unsat |
| NDT Witnessing: The following questions are to be answered as a result of observing NDT being performed and/or observation of the applicable work area: |  |
| Magnetic Particle (MT): ___Sat ___Unsat ___N/A ___Witnessed ___Review of Records |  |
| 8. | Is the correct procedure readily available to the inspector? | ___Yes ___No |
|  | b. Is performance in accordance with the method/set-up of the procedure? (Unidirectional vice multidirectional) | ___Yes ___No |
| 9. | Is the inspector qualified? | ___Yes ___No |
| 10. | Is the amperage within the procedure range? | ___Yes ___No ___N/A |
| 11. | Is the lighting adequate per procedure? | ___Yes ___No ___N/A |
| 12. | Are correct accept/reject criteria being applied? | ___Yes ___No ___N/A |
| 13. | Do inspection records indicate heat off date when required? (For 24 hour or 7 day MT)? | ___Yes ___No ___N/A |
| 14. | Are records of MT performed adequate i.e. inspector and date, joint or piece inspected, equipment used, number and type of defects, repair description? | ___Yes ___No ___ N/A |
| 15. | Is equipment calibration current? | ___Yes ___No ___N/A |
| 16. | Is material being demagnetized after testing, as required by procedure? | ___Yes ___No |
| Liquid Penetrant (PT): ___Sat ___Unsat ___N/A ___Witnessed ___Review of Records |  |

| 17. | a. Is the correct procedure available to the inspector? | ___Yes ___No |
| --- | --- | --- |
|  | b. Is performance in accordance with the procedure? | ___Yes ___No |
| 18. | Is the inspector qualified? | ___Yes ___No |
| 19. | Is the lighting adequate per procedure? | ___Yes ___No ___N/A |
| 20. | Are correct accept/reject criteria being applied? | ___Yes ___No |
| 21. | Is the proper test method being utilized for the type of inspection being performed i.e. Group I for welds, other than Group I for fasteners? | ___Yes ___No |
| 22. | a. Are the penetrant materials used as listed in the approved procedure (cleaners, penetrants, solvent, developer)? | ___Yes ___No |
|  | b. Are penetrant materials traceable to the certifications? | ___Yes ___No |
| 23. | Are the correct precleaning, penetrant and inspection developer dwell times being used? | ___Yes ___No |
| 24. | Is proper post inspection cleaning of the part performed? | ___Yes ___No ___N/A ___ Not Observed |
| 25. | Are there adequate records of PT performed? | ___Yes ___No |
| Radiography (RT): ___Sat ___Unsat ___N/A ___Witnessed ___Review of Records |  |
| 26. | a. Is the correct procedure readily available to the inspector? | ___Yes ___No |
|  | Is performance in accordance with the method/set-up of the procedure? | ___Yes ___No |

| 27. | Is a sketch, drawing, procedure or equivalent record available to show the set-up used to make each radiograph? | ___Yes ___No |
| --- | --- | --- |
|  | b. Is the sketch, drawing or procedure legible? | ___Yes ___No |
| 28. | Is there a system for positive identification of RT film correlating to the part inspected? | ___Yes ___No |
| 29. | Are the RT location markers maintained on the part to permit coordination with their images on the film? | ___Yes ___No ___N/A |
| 30. | Is the film viewing facility constructed to exclude objectionable background lighting and contain a film viewed with a cooling device and densitometer? | ___Yes ___No |
| 31. | Are penetrameters correctly identified with lead numbers or engraved strips indicating material thickness? | ___Yes ___No |
| 32. | Are penetrameters permanently identified by material or principal alloy? | ___Yes ___No |
| 33. | Is the correct penetrameter being used? | ___Yes ___No |
| 34. | Are appropriate calculations of source half-life/exposure time being performed? | ___Yes ___No |
| 35. | Are radiographic film storage areas adequate? | ___Yes ___No ___N/A |
| 36. | Are radiographic film packages adequately maintained? (i.e. torn, wet damaged) | ___Yes ___No ___N/A |
| 37. | Are all artifacts identified and dispositioned on the reader sheet? | ___Yes ___No ___N/A |
| 38. | Do RT records contain the following: | ___Yes ___No |
|  | Correct penetrameter size used | ___Sat ___Unsat ___N/A |
|  | b. Correct penetrameter material used | ___Sat ___Unsat ___N/A |
|  | c. Proper shim material and thickness used | ___Sat ___Unsat ___N/A |
|  | Correct source-to-film distance used | ___Sat ___Unsat ___N/A |
|  | e. Film density on block image is not greater than 15% of the density in area of interest | ___Sat ___Unsat ___N/A |
|  | f. Film density (single film viewing) is 1.5 to 4.0 in area(s) to be examined | ___Sat ___Unsat ___N/A |
|  | g. Film density (double film viewing) is 1.5 to 4.0 in area(s) to be examined | ___Sat ___Unsat ___N/A |
|  | h. Radiograph(s) show complete coverage | ___Sat ___Unsat ___N/A |
|  | i. Complete coverage of repaired area(s) | ___Sat ___Unsat ___N/A |
|  | j. Original radiographs of repaired area(s) included with overread package if applicable) | ___Sat ___Unsat ___N/A |
|  | k. RSS provided with overread package | ___Sat ___Unsat ___N/A |
|  | l. Shooting sketch specifies wall thickness of item | ___Sat ___Unsat ___N/A |
|  | m. Sketch (es) showing location(s), size(s), shape(s) of repaired area(s) included with over read package | ___Sat ___Unsat ___N/A |
|  | n. Film processing defects and artifacts have been | ___Sat ___Unsat ___N/A |
|  | o. Radiographic Inspection Report has Contractor Approval when required by the purchase order/contract | ___Sat ___Unsat ___N/A |
| Ultrasonic Inspection (UT): ___Sat ___Unsat ___N/A ___Witnessed ___Review of Records |  |
| 39. | a. Is the correct procedure readily available to the inspector? | ___Yes ___No |
|  | b. Are performance and methods/set-up in accordance with the procedure? (longitudinal vice transverse) | ___Yes ___No |
| 40. | Is the inspector qualified? | ___Yes ___No |
| 41. | Is a system in place to qualify equipment, including master transducers and calibration blocks? | ___Yes ___No |
| 42. | Is the surface finish of the piece being tested in accordance with the procedure? | ___Yes ___No ___N/A |
| 43. | Is the calibration block/s correctly identified by material type and uniquely identified (serialized)? | ___Yes ___No ___N/A |
| 44. | Is the couplant removed at the completion of testing? | ___Yes ___No ___N/A ___ Not Observed |
| 45. | a. Is calibration checked/rechecked at the beginning and completion of testing? | ___Yes ___No ___N/A |
|  | b. Is equipment calibration current? | ___Yes ___No |
| 46. | Are inspection records adequate? | ___Yes ___No |
| Eddy Current Inspection (ET): ___Sat ___Unsat ___N/A ___Witnessed ___Review of Records |
| 47. | Is the correct procedure available to the inspector? | ___Yes ___No |
|  | b. Is performance in accordance with the procedure? | ___Yes ___No ___N/A |
| 48. | Is the inspector qualified? | ___Yes ___No |
| 49. | Is the surface finish/configuration of the part adequate to allow free movement of the probe? | ___Yes ___No ___N/A |
| 50. | Is the calibration standard utilized by material type and uniquely identified? | ___Yes ___No |
| 51. | Is the instrumentation used calibrated as required by procedure? | ___Yes ___No |
| 52. | Is the frequency setting correct for the probe used? | ___Yes ___No |
| 53. | Is the scanning technique and speed in accordance with the procedure? | ___Yes ___No |
| 54. | Are ET rejectable indications being dispositioned properly (i.e., ET rejects verified by MT)? | ___Yes ___No |
| 55. | Are inspection records adequate to meet procedural requirements? | ___Yes ___No |
| Visual Inspection (VT): ___Sat ___UnSat N/A ___Witnessed ___Review of Records |
| 56. | a. Is the correct procedure readily available to the inspector? | ___Yes ___No |
|  | b. Is performance in accordance with the procedure? | ___Yes ___No |
|  | c. When applicable, is the correct magnification used? | ___Yes ___No |
| 57. | Is the inspector qualified? | ___Yes ___No |
| 58. | Are adequate gages and measuring devices available to perform inspection in accordance with the procedure? | ___Yes ___No ___N/A |
| 59. | Is lighting adequate? | ___Yes ___No |
| 60. | For VT of welds, do inspections and records adequately cover the cover the following: |  |
|  | * Weld size ______________ | ___Yes ___No |
|  | * Weld configuration ______________ | ___Yes ___No |

|  | * Surface uniformity ______________ | ___Yes ___No |
| --- | --- | --- |
|  | * Surface cleanliness ______________ | ___Yes ___No |
|  | * Physical defects ______________ | ___Yes ___No |
|  | * Contour of welded and/or ground surface ______________ | ___Yes ___No |
| 61. | For VT of items other than welds, are records available? | ___Yes ___No |

Additional Comments/Concerns: