NOTE - ALL QUESTIONS ON THIS AUDITOR'S PROCESS GUIDE IS CONSIDERED TO BE PRIORITY CODE "A"

| 1. | a. Identify types of heat treatment performed at your facility being audited: |  |
| --- | --- | --- |
|  | ___Homogenize | ___Stress Relief | ___Normalize |  |
|  | ___Heat Soak | ___Anneal | ___Tempering/Quenching |  |
|  | ___Age Hardening |  |  |
|  | ___Other (Specify): |  |
|  | b. Is heat-treating performed to written procedures? | ___Yes ___No ___N/A |
|  | c. Is it readily available to the operator? | ___Yes ___No ___N/A |
| 2. | Are the heat treatment operations performed by a continuous process or individual furnace loads? |  |
|  | ___Continuous | ___Individual | ___Furnace Load | ___N/A |
| 3. | If a continuous process is used, describe fully, using specific equipment identifications (e.g. model numbers): | ___N/A |

|  | Identify heat source type: |  |
| --- | --- | --- |
|  | Location: |  |
|  | Controls: |  |
|  | Placement of temperature monitoring equipment (i.e. thermocouples): |  |
| 4. | If individual furnace loads are heat treated, describe: | ___N/A |
|  | a. Furnace type (e.g. car bottom, front load or side load). Include make or model number if possible: |  |
|  | b. Burner controls, including method of on/off switching: |  |

|  | c. Placement of temperature sensors (thermocouples): In oven On Product |  |
| --- | --- | --- |
|  | d. Method of loading furnace/s: |  |
|  | e. Method of unloading furnace/s: |  |
|  | f. Method of cooling, including transport to cooling location: |  |
|  | g. Does the furnace have sufficient temperature sensing devices to insure uniform furnace temperature? | ___Yes ___No ___N/A |
| 6. | Does supplier's procedures address fuel source's requirements? | ___Yes ___No ___N/A |
| 7. | a. Do supplier's equipment contain mercury? | ___Yes ___No ___N/A |
|  | b. Is it identified? | ___Yes ___No ___N/A |

|  | c. Are necessary controls in place to prevent contamination of the part? | ___Yes ___No ___N/A |
| --- | --- | --- |
| 8. | Do the procedures contain parameters, which meet applicable specifications (e.g. MIL-H-6875, MIL-STD-1684) for time and temperature? | ___Yes ___No ___N/A |
| 9. | Is a traveler or equivalent work process control document utilized? | ___Yes ___No ___N/A |
| 10. | Does the work process control document contain requirements for time, temperature, cooling methods and documentation requirements? | ___Yes ___No ___N/A |
| 11. | a. Are time at temperature charts produced? If not, describe alternative control/s used: | ___Yes ___No ___N/A |
|  | b. Are the at-temperature charts traceable to the material? | ___Yes ___No ___N/A |
| 12. | a. What is the method utilized to confirm successful heat treat to specific required mechanical properties (hardness, tensile testing, etc.). | ___N/A |
|  | b. Does this method meet the specified requirement? | ___Yes ___No |
|  | c. Does the procedure ensure test coupons are heat treated together with the material? | ___Yes ___No ___N/A |
| 13. | Does the procedure document the process for resolving nonconformance on heat-treated material? | ___Yes ___No ___N/A |
| 14. | Does the supplier have a system for calibration of the temperature control equipment? (E.g. controller, thermocouple, lead wire): | ___Yes ___No ___N/A |
| 15. | Are heat treating equipment and test equipment (including hardness testing) identified in a manner to reflect (ISO 4.11.1)? |  |
|  | a. Personnel responsible for performing calibration inspection? | ___Yes ___No ___N/A |
|  | b. Personnel responsible for calibration/inspection. | ___Yes ___No ___N/A |
|  | c. Item identity or serial number. | ___Yes ___No ___N/A |
|  | d. Is calibration current? | ___Yes ___No ___N/A |
|  | f. If calibration is subcontracted, are sufficient subcontractor controls in place? | ___Yes ___No ___N/A |
| HEAT TREAT OVEN SURVEY (MIL-STD-1684) | ___Yes ___No ___N/A |

| 16. | Does the supplier have a system for heat treat oven/furnace survey? | ___Yes ___No ___N/A |
| --- | --- | --- |
| 17. | Has the survey been performed at the correct time interval? | ___Yes ___No ___N/A |
| 18. | Has it been done at the correct temperature? | ___Yes ___No ___N/A |
| WITNESS HEAT TREAT WORK IN PROCESS AND RESPOND TO THE FOLLOWING: | ___Not Observed ___Sat ___Unsat ___N/A |
|  | Record number of samples reviewed: _________ |  |
| 19. | Is/Are the furnaces and controllers calibrated? | ___Sat ___Unsat ___N/A |
| 20. | Is the temperature correct? | ___Sat ___Unsat ___N/A |
| 21. | Is the correct cooling method/medium being utilized? | ___Sat ___Unsat ___N/A |
| 22. | Are personnel cognizant of parameters (time, temperature, cooling method) required by procedure/s and work instructions? | ___Sat ___Unsat ___N/A |

| 23. | Are results being properly documented (furnace charts)? | ___Sat ___Unsat ___N/A |
| --- | --- | --- |
| 24. | Are heat treat procedures/work control documents readily available to operators? | ___Sat ___Unsat ___N/A |
| 25. | Is traceability being maintained and is the material being heat-treated identified by heat number, batch number, serial number or equivalent to assure material control and prevent material mix up? | ___Sat ___Unsat ___N/A |
| 26. | Are test coupons being heat-treated together with the material? | ___Sat ___Unsat ___N/A |

# Additional Comments/Concerns: