MASS DEACIDIFICATION PILOT PROJECT

The pilot project to evaluate the Bookkeeper process for mass deacidification was carried out in two phases.  The first phase was a survey of the NLM post 1800 collection to determine how many volumes were suitable for treatment with the Bookkeeper process.  The second phase consisted of deacidification treatment of 184 volumes and an evaluation of the results.

- DEACIDIFICATION  PROCESS

The Bookkeeper deacidification process treats materials in small batches.  Bound volumes are fanned open on specially designed racks that are placed in tanks.  The deacidification liquid, magnesium oxide suspended in perfluoralkane, is pumped into the tank and submerses them for about 30 minutes.  Gentle motions of the paper and liquid are used to help to ensure uniform coverage.  The treating bath is continuously circulated to filter loose dust and dirt from the books and to monitor and maintain the proper concentration of treating materials.  All unused perfluoralkane is then evicted from the tank and recovered, making the process both environmentally friendly and economically efficient.  A vacuum is pulled into the tank to aid the drying process.  A batch usually takes about 2 hours.  Because the treatment does not use water or other solvents, inks, bookcloth, and glues are not damaged in the process.

Very small particles (about 1 micron) of magnesium oxide are deposited into the structure of the paper.  In the first few weeks following treatment, the magnesium oxide particles combine with moisture in the air to form magnesium hydroxide, a non-toxic alkaline reserve.  The particles that make up the alkaline reserve readily absorb and neutralize the acids in the paper and continue to absorb acid over the life of the paper.  This has been demonstrated by accelerated aging tests and tests done with books treated over the past eight years.  These tests have shown that treatment by the Bookkeeper process should extend the usable life of paper based materials 3 to 5 times.   The Bookkeeper process is already being used to deacidify about 200,000 volumes and 3,750 cubic feet of manuscript or archival material per year from 40 research libraries.  The Library of Congress recently announced plans to increase the number of volumes they send for treatment from 100,000 to 300,000 per year.

Not all acidic materials are suitable for treatment by Bookkeeper. The Bookkeeper process is not as effective with coated paper.  The magnesium hydroxide remains on the coating and does not react with the acids in the paper.  The small chamber size also places size limitations on the volumes treated though new treatment tanks make it possible to treat larger volumes and manuscripts in a separate processing stream. Volumes must be structurally intact to be put on the racks and subjected to the movement of the fluids in the tanks.  The process does not strengthen already brittle paper.  Therefore, filmed, already brittle, and damaged volumes are also not suitable for treatment.

Book Rack					 Deacidification Treatment Tanks

System of Tanks

II.	COLLECTION SURVEY

The survey was necessary to identify what portion of the collection could be treated and to help set priorities for treatment.   A survey of the collection was designed to gather data needed for making selection decisions.  One thousand volumes were surveyed.  Volumes were surveyed from six subcollections, the same subcollections included in an earlier study of brittleness done in 1987.  These subcollections were:  Serials published 1989 to present, classed W1 (B1), Serials published 1914 to present, classed other than  W1 (B2),  Serials published 1871-1989, classed W1 (B3), Monographs published 1914 to present (B2), Serials published 1801-1870 (HMD), and Monographs published 1801-1914 (HMD).  Random numbers were generated to select a particular volume from a particular shelf within each collection area.

During the week of August 21-25, two employees of Bookkeeper pulled and examined volumes and recorded data for the survey.   The following data were collected about each volume and input into an Access database:

Bibliographic/Identification:  Title, call number, date,  country of publication, item barcode, collection location

Size:  Height, width, thickness, weight

Physical condition: Binding style, acid or alkaline paper as measured by a pH testing pen, coated or calendared paper, brittleness as measured by foldtest, damage

## Volumes Suitable for Deacidification

| Collection Location | Percent of Subcollection | Number of Volumes |
| --- | --- | --- |
|  | Uncoated | Slightly Glossy | Uncoated | Slightly Glossy |
| Serials B1 (1990-2001) | 5.8% | 5.2% | 19,490 | 17,470 |
| Serials B2 (1914- 2001) | 52.0% | 18.0% | 50,440 | 17,460 |
| Serials B3 (1871-1989) | 21.1% | 17.3% | 161,630 | 132,520 |
| Serials HMD (1801-1870) | 28.6% | 4.8% | 11,330 | 1,900 |
| Monographs B2 (1914-2001) | 40.9% | 14.7% | 249,490 | 89,670 |
| Monographs HMD (1801-1913) | 37.3% | 3.9% | 37,300 | 3,900 |
| Total |  |  | 529,680 | 262,920 |

Survey results indicate that approximately 529,680 volumes or 27.2% of the surveyed collection are acidic, not brittle and on uncoated paper.  The treatment of these volumes should be fairly straightforward. The NLM has much coated paper, but early coated paper is not as thickly coated and is only slightly glossy. For the survey purposes, coated paper was categorized as either heavily coated or slightly glossy . There were an additional 262,920 volumes (13.5% of the collection) that are acidic, not yet brittle and on slightly glossy paper.  We have discussed the treatment of the slightly glossy paper with Bookkeeper and they are planning to test new processes so that such volumes can be treated successfully.

Survey results show a significant decline in the amount of acid paper acquired in the collection since the mid 1980’s.  However, 12.1% of materials received since 1996 were found to be on acidic paper.

Another relevant finding of the survey was that 12% (233,832 volumes) were brittle.  This represents 65,832 more brittle volumes than were brittle in 1985.   This means that almost 4,500 volumes are becoming brittle each year.   The cost of microfilming is over $180.00 per volume, the cost of deacidification is about $18.00 per volume.  The cost of microfilming the 4,500 volumes that will become brittle in one year is over $ 729,000 more than deacidifying them before they become brittle.  The cost of microfilming the 800,000 volumes destined to become brittle is $144 million  while the cost of deacidifying them before they become brittle is $14.4 million.

III.	DEACIDIFICATION RESULTS

The second phase of the Mass Deacidification pilot study was to select volumes for deacidification and send them to Bookkeeper.  The procedures and specifications were similar to those envisioned for a larger contract. The purpose of this phase was to test the logistical procedures for handling and shipping and to determine whether the Bookkeeper process was effective and non-damaging.  The effectiveness of the treatment was based on the resulting alkaline reserve and the change in pH before and after treatment.

For the sample we selected acidic volumes in good condition from titles in the original sample population.  We did this because we had already collected data about their physical characteristics and condition.  A Bookkeeper staff member who selects volumes for deacidification at the Library of Congress reviewed our selections to make sure they would not incur damage and packed them for shipment in the Bookkeeper totes.  One hundred and eighty volumes were selected from the sample.

To determine how slightly glossy volumes would respond to treatment, I took additional volumes that were slightly glossy to the Bookkeeper facility in October before the deacidification was done to discuss how they might be handled.  We agreed to deacidify four of those to evaluate their post treatment condition.  In all, 184 volumes were deacidified.

The pH of the volumes was measured before and after treatment with a Fisher Scientific Accumet pH meter.  I visited Bookkeeper prior to the treatment of the volumes to learn how Bookkeeper measured the pH so that the readings taken at NLM after treatment would be consistent with those done by Bookkeeper. The volumes sent were determined to be acidic on the basis of a test with a pH testing pen containing Chlorophenol red indicator solution.  This test can be unreliable on coated or colored paper.   During our pretreatment pH testing using the Accument meter, nineteen volumes were found to be non acidic (above pH 6.8).  We went ahead with deacidification, but noted that we may need to evaluate the readings we get from pH pens for certain paper types.   These volumes will be excluded from this report. The pH readings of the remaining 165 volumes prior to treatment ranged from 2.84 to 6.65  (Average: pH: 4.5).

Besides recording the pH tests, the Bookkeeper staff again examined the volumes to make sure they could be treated without damage.  They documented instances of minor damage existing prior to treatment.

The volumes were deacidified and returned to NLM in November.  In late January and early February, I did pH testing of all the deacidified volumes.  The tests were not performed immediately after deacidification because the treatment reaction continues  for some time after the deposit of the alkaline materials in the book.  The Library of Congress specifies that the pH of deacidified books should be between 6.8 and 10.4.    The pH readings for the NLM sample after treatment ranged from 6.41 to 10.32.  The average pH of treated volumes was 9.3.  The pH of all volumes increased at least 1.77.   The average increase in pH was 4.9.  See attached table for pH readings before and after the treatment.

There were only 3 volumes where the resulting pH was below 6.8 or showed less than 2 points increase.  Further testing showed that all 3 volumes had significantly higher (all over 9.2) pH readings on another page within the book.  This is due to variations in the paper within the volume and uneven distribution of the alkaline particles.  It has been shown that acids migrate toward the areas of the alkaline particles so that once treated the acids throughout such volumes eventually will become neutralized.

The alkaline reserve is a measure of the amount of treatment materials deposited in the paper.  Library specifications for minimum alkaline reserve range from 1.0 to 1.5.

To test for consistency of treatment among treatment batches, Bookkeeper placed sheets of neutral Watman paper in volumes so that 5% of the treating chambers used for the shipment were tested.  The test papers were cut into two equal parts.  The Contractor tested one half of the batch of test papers and reported the results to NLM and returned the other half of the papers to NLM for independent testing. In the test papers the alkaline reserve ranged from 1.2-1.7 and the pH ranged from 9.8-10.0.   No further testing for alkaline reserve was done, as this test requires destroying the paper.

I examined the volumes when unpacking and again in more detail when performing the pH tests.  I found no damage caused by the mass deacidification treatment or the Bookkeeper handling of the volumes. One or two of the buckram covers felt tacky.  This is due to a reaction with oils used in the production of some pyroxylin coatings of book cloths.  Bookkeeper has a method of wiping off this residue from the cover.

It must be noted that the treated volumes do have a slightly different feel to the paper.  There is a slight residue that leaves a dusty feel to some types of paper.  More of this residue is left on glossy pages but Bookkeeper wipes these pages and the covers off as a matter of course.  The four slightly glossy volumes were intentionally not wiped, but the residue did not seem to be more noticeable than that found on other volumes. While I do not find the feel of the treated books unacceptable, it is likely to be noticed by some users.

A label was applied to the inside of the back of the volume which recorded: name and address of the company providing deacidification services, the name of the deacidification process, identification of the neutralizing agent employed, and the date of the treatment. Also a small dot was placed at the bottom of each volume to give a quick visual reference that the book was treated.  In addition to the labeling of the piece, the Voyager item record will be updated to indicate that the volume has been deacidified so that we can generate reports and test for changes in pH in future years.

IV.	RECOMMENDATIONS

Almost 800,000 volumes in the NLM collection are printed on acidic paper that could benefit from deacidification using the Bookkeeper process.  The life of these volumes would be extended 3 to 5 times and $130 million dollars in microfilming costs would be saved  by instituting a program of deacidification.  We are proposing a program to deacidify the acidic volumes in the NLM collection over a period of  25 years.   The project would be phased in.  Ten thousand volumes would be deacidifed in the first year of a five year contract.  By the final year maximum production of 40,000 volumes would be achieved.  This would cost $180,000 for the first year, increasing to approximately $720,000 per year when fully funded.  The estimated contract cost includes processing activities onsite at NLM by Bookkeeper.   Bookkeeper personnel would select, pack, ship, check in and update records for the volumes at NLM.  As part of the selection for treatment review, information about the volumes examined, such as brittle paper, damage, etc., will be collected and available for use in selecting materials for other preservation activities.

As is the case for microfilming brittle volumes, priority for deacidification would be given to serials indexed in Index Medicus and its precursors. Higher priority would be given to older serials in HMD and B3 stacks area because they will become brittle much sooner than more recent serials.  Slightly glossy paper should be included in the project, but we would closely monitor results and revise selection criteria as necessary to make sure we are selecting those that benefit from treatment. Selecting the slightly glossy paper that can be treated now is more efficient than making another pass through the collection to identify it later.   A sample of new acquisitions should be tested for acidity on a regular basis to determine whether a high percentage of medical publications continue to be printed on alkaline paper and to identify titles that will need treatment in the future.  Both volumes and records would be labeled to indicate that the volumes were deacidified.  Close monitoring of treated volumes by pH testing upon receipt and at 5 year intervals will assure us of the efficacy of the process.

pH BEFORE AND AFTER TREATMENT

| Call Number | Year | pH Before | pH After | Difference in pH |
| --- | --- | --- | --- | --- |
| 1995 C-851 | 1994 | 6.51 | 10.17 | 3.66 |
| 1995 J-244 | 1994 | 4.71 | 9.33 | 4.62 |
| 2000 D-473 | 1997 | 6.15 | 10.04 | 3.89 |
| AA6430 | 1981 | 4.81 | 9.25 | 4.44 |
| AA8378 | 1982 | 4.47 | 9.64 | 5.17 |
| B591 | 1974 | 4.38 | 9.55 | 5.17 |
| BF 371 F691L 1965 | 1965 | 4.15 | 10.02 | 5.87 |
| DD5642 | 1984 | 4.59 | 9.59 | 5.00 |
| E150 | 1967 | 4.87 | 9.05 | 4.18 |
| EE3483 | 1979 | 4.44 | 9.88 | 5.44 |
| EE6184 | 1985 | 4.89 | 9.47 | 4.58 |
| EE6758 | 1985 | 3.97 | 8.98 | 5.01 |
| EE7206 | 1986 | 4.91 | 8.52 | 3.61 |
| F671 | 1967 | 3.91 | 8.81 | 4.90 |
| F814 | 1978 | 6.20 | 9.94 | 3.74 |
| GG3799 | 1972 | 4.61 | 8.51 | 3.90 |
| GG5290 | 1988 | 4.39 | 7.09 | 2.70 |
| HA 201 G326 1980 | 1980 | 4.31 | 9.12 | 4.81 |
| HV 2430 N277f 1967 | 1967 | 5.16 | 10.02 | 4.86 |
| QH 405 P779d 1974 | 1974 | 4.49 | 9.70 | 5.21 |
| QH 581 G139a 1957 | 1957 | 3.37 | 9.44 | 6.07 |
| QT 180 B534e 1948 | 1948 | 3.83 | 9.24 | 5.41 |
| QT 265 S871n 1953 | 1953 | 3.86 | 9.92 | 6.06 |
| QV 132 M466v 1952 | 1952 | 4.19 | 9.50 | 5.31 |
| QW 4 F699m 1976 | 1976 | 4.04 | 9.83 | 5.79 |
| QZ 202 M119c 1954 | 1954 | 4.91 | 9.96 | 5.05 |
| T479 | 1967 | 3.87 | 9.56 | 5.69 |
| W 19 B879g 1978 | 1978 | 4.45 | 10.03 | 5.58 |
| W 275 FA1 M18 1982 | 1982 | 4.22 | 9.79 | 5.57 |
| W1 A1138K | 1974 | 4.31 | 9.48 | 5.17 |
| W1 AC422 | 1974 | 5.07 | 9.43 | 4.36 |
| W1 AC863B | 1969 | 4.89 | 10.02 | 5.13 |
| W1 AC9553 | 1982 | 4.80 | 9.40 | 4.60 |
| W1 AC982 | 1978 | 4.94 | 9.41 | 4.47 |
| W1 AD115F | 1988 | 4.85 | 9.79 | 4.94 |
| W1 AM352 | 1976 | 4.60 | 9.54 | 4.94 |
| W1 AN231 | 1982 | 4.76 | 9.59 | 4.83 |
| W1 AN77 | 1956 | 3.90 | 8.73 | 4.83 |
| W1 AR231 | 1921 | 4.30 | 8.86 | 4.56 |
| W1 AR255 | 1922 | 4.43 | 10.01 | 5.58 |
| W1 AR255 | 1923 | 4.48 | 10.05 | 5.57 |
| W1 AR255 | 1923 | 4.74 | 9.92 | 5.18 |
| W1 BI451 | 1978 | 4.71 | 9.28 | 4.57 |
| W1 BI672 | 1985 | 4.47 | 7.49 | 3.02 |
| W1 BI754L | 1977 | 4.80 | 10.09 | 5.29 |
| W1 BI876M | 1996 | 4.23 | 9.49 | 5.26 |
| W1 BI876M | 1996 | 4.86 | 9.70 | 4.84 |
| W1 BU842 | 1988 | 4.11 | 9.55 | 5.44 |
| W1 CH982AB | 1986 | 4.49 | 9.71 | 5.22 |
| W1 CU132I | 1972 | 4.34 | 9.21 | 4.87 |
| W1 EK283 | 1979 | 4.29 | 9.36 | 5.07 |
| W1 EU446 | 1961 | 4.91 | 9.52 | 4.61 |
| W1 FO128R | 1974 | 5.09 | 8.98 | 3.89 |
| W1 FO22 | 1980 | 5.10 | 9.65 | 4.55 |
| W1 FO685I | 1983 | 4.42 | 10.31 | 5.89 |
| W1 HE4705 | 1974 | 5.02 | 9.59 | 4.57 |
| W1 HU426 | 1969 | 3.71 | 8.88 | 5.17 |
| W1 I245 | 1968 | 4.91 | 10.21 | 5.30 |
| W1 JA205DK | 1915 | 4.61 | 9.49 | 4.88 |
| W1 JO212 | 1975 | 2.84 | 9.20 | 6.36 |
| W1 JO212 | 1975 | 3.83 | 9.70 | 5.87 |
| W1 JO674D | 1951 | 4.53 | 10.02 | 5.49 |
| W1 JO674D | 1952 | 3.83 | 8.88 | 5.05 |
| W1 JO874 | 1983 | 4.07 | 10.17 | 6.10 |
| W1 JO874 | 1984 | 4.32 | 9.95 | 5.63 |
| W1 JO939P | 1969 | 3.94 | 8.56 | 4.62 |
| W1 JO939P | 1969 | 4.35 | 10.04 | 5.69 |
| W1 JO966C | 1988 | 4.38 | 9.51 | 5.13 |
| W1 JO966C | 1988 | 4.53 | 8.28 | 3.75 |
| W1 KA411H | 1974 | 3.93 | 8.74 | 4.81 |
| W1 KA411H | 1974 | 4.02 | 9.07 | 5.05 |
| W1 KH45 | 1983 | 3.43 | 7.68 | 4.25 |
| W1 KH45 | 1983 | 3.73 | 9.43 | 5.70 |
| W1 KO282N | 1988 | 4.38 | 9.60 | 5.22 |
| W1 KO282N | 1988 | 4.50 | 6.41 | 1.91 |
| W1 KY9927 | 1994 | 3.55 | 9.40 | 5.85 |
| W1 KY9927 | 1996 | 3.73 | 9.35 | 5.62 |
| W1 LE334N v.14 1981 | 1981 | 4.53 | 9.12 | 4.59 |
| W1 LE955 | 1974 | 3.92 | 10.13 | 6.21 |
| W1 LE955 | 1975 | 3.88 | 9.74 | 5.86 |
| W1 LI62 | 1939 | 3.80 | 9.33 | 5.53 |
| W1 LI62 | 1940 | 4.05 | 9.33 | 5.28 |
| W1 ME15 | 1964 | 4.24 | 6.82 | 2.58 |
| W1 ME15 | 1964 | 5.09 | 9.52 | 4.43 |
| W1 ME158Q | 1979 | 4.60 | 9.70 | 5.10 |
| W1 ME158Q | 1981 | 4.71 | 9.53 | 4.82 |
| W1 NA944N | 1968 | 4.71 | 8.66 | 3.95 |
| W1 NA944N | 1969 | 4.42 | 9.86 | 5.44 |
| W1 NE204 | 1982 | 4.19 | 9.18 | 4.99 |
| W1 NE204 | 1983 | 4.55 | 10.31 | 5.76 |
| W1 NI928M | 1960 | 3.76 | 6.86 | 3.10 |
| W1 NI928M | 1960 | 3.88 | 9.24 | 5.36 |
| W1 OR877 | 1976 | 3.96 | 9.48 | 5.52 |
| W1 OR877 | 1976 | 4.11 | 7.23 | 3.12 |
| W1 PA968 | 1976 | 3.76 | 6.57 | 2.81 |
| W1 PA968 | 1976 | 4.95 | 9.71 | 4.76 |
| W1 PR242 | 1978 | 3.64 | 8.68 | 5.04 |
| W1 PR242 | 1978 | 3.75 | 9.19 | 5.44 |
| W1 PR242 | 1981 | 3.37 | 9.26 | 5.89 |
| W1 PR242 | 1981 | 3.40 | 9.39 | 5.99 |
| W1 PR577K | 1977 | 4.22 | 9.44 | 5.22 |
| W1 PR577K | 1977 | 4.30 | 10.32 | 6.02 |
| W1 RO991 | 1956 | 3.51 | 8.39 | 4.88 |
| W1 SC642R | 1985 | 5.00 | 9.34 | 4.34 |
| W1 SO104H | 1977 | 5.11 | 9.64 | 4.53 |
| W1 SO104H | 1978 | 4.95 | 9.10 | 4.15 |
| W1 ST439 | 1972 | 4.96 | 9.67 | 4.71 |
| W1 ST439 | 1975 | 4.61 | 10.11 | 5.50 |
| W1 TE637 | 1980 | 4.87 | 9.80 | 4.93 |
| W1 TE637 | 1980 | 4.90 | 9.32 | 4.42 |
| W1 TS278B | 1985 | 3.91 | 8.31 | 4.40 |
| W1 TS278D | 1966 | 3.99 | 9.28 | 5.29 |
| W1 UN101H | 1983 | 4.51 | 9.63 | 5.12 |
| W1 UN101H | 1984 | 4.93 | 9.67 | 4.74 |
| W1 VE821 | 1991 | 4.36 | 9.86 | 5.50 |
| W1 VE821 | 1991 | 4.45 | 9.35 | 4.90 |
| W1 VE841 | 1974 | 3.29 | 9.03 | 5.74 |
| W1 VE841 | 1975 | 4.10 | 9.92 | 5.82 |
| W1 VO6405 | 1992 | 4.17 | 8.09 | 3.92 |
| W1 VO6405 | 1992 | 4.22 | 7.01 | 2.79 |
| W1 WE998 | 1972 | 4.68 | 9.02 | 4.34 |
| W1 WE998 | 1973 | 5.04 | 9.28 | 4.24 |
| W1 YA444M | 1985 | 5.13 | 9.51 | 4.38 |
| W1 YA444M | 1987 | 5.11 | 9.21 | 4.10 |
| W1 ZA766 | 1996 | 4.29 | 10.05 | 5.76 |
| W1 ZA766 | 1997 | 4.33 | 9.11 | 4.78 |
| W1 ZU787 | 1967 | 4.72 | 10.03 | 5.31 |
| W1 ZU787 | 1967 | 5.07 | 9.54 | 4.47 |
| W3 C484 | 1948 | 3.80 | 9.44 | 5.64 |
| W3 LI435P 1964d | 1964 | 4.45 | 9.39 | 4.94 |
| W3 NA439N 1973f | 1973 | 5.33 | 10.03 | 4.70 |
| W3 NU36 no.12 1983 | 1983 | 4.88 | 9.66 | 4.78 |
| WA 18 U573he 1958 | 1958 | 4.21 | 9.54 | 5.33 |
| WA 30 D584a 1976 | 1976 | 3.69 | 9.85 | 6.16 |
| WA 300 U58r 1985 | 1985 | 5.46 | 9.63 | 4.17 |
| WA 390 L614p 1970 | 1970 | 4.18 | 9.93 | 5.75 |
| WB 143 S293m 1968 | 1968 | 3.72 | 8.89 | 5.17 |
| WB 430 M434i 1975 | 1975 | 3.91 | 9.35 | 5.44 |
| WD 308 M4887 1987 | 1987 | 4.87 | 9.28 | 4.41 |
| WD 712 R399t 1966 | 1966 | 4.23 | 9.80 | 5.57 |
| WG 140 M359r 1976 | 1976 | 4.33 | 9.34 | 5.01 |
| WM 270 S933 1974 | 1974 | 3.79 | 9.82 | 6.03 |
| WM 400 Z43i 1928 | 1928 | 4.49 | 8.33 | 3.84 |
| WM 412 E375 1985 | 1985 | 4.14 | 9.82 | 5.68 |
| WM 420 P778g 1973 | 1973 | 4.36 | 7.93 | 3.57 |
| WM 420 W848t 1967 | 1967 | 4.01 | 8.88 | 4.87 |
| WM 460 C456 1978 | 1978 | 5.24 | 9.83 | 4.59 |
| WM 475 A313f 1967 | 1967 | 4.18 | 8.11 | 3.93 |
| WM 615 F889h 1962 | 1962 | 3.69 | 9.66 | 5.97 |
| WO 192 R751m 1944 | 1944 | 4.30 | 9.81 | 5.51 |
| WO 75 P944 1980 | 1980 | 6.58 | 8.35 | 1.77 |
| WS 107 B264m 1974 | 1974 | 3.89 | 9.82 | 5.93 |
| WX 150 P459e 1969 | 1969 | 4.05 | 9.51 | 5.46 |
| WX 157 B393b 1980 | 1980 | 4.19 | 10.11 | 5.92 |
| WX 159 R167w 1978 | 1978 | 5.20 | 9.52 | 4.32 |
| WY 159 W872c 1981 | 1981 | 6.65 | 9.73 | 3.08 |
| WY 20.5 R357r 1987 | 1987 | 5.29 | 10.04 | 4.75 |
| WY 26.5 C7365 1981 | 1981 | 4.37 | 9.43 | 5.06 |
| WZ 100 M8918M 1969a | 1969 | 4.92 | 9.90 | 4.98 |
| WZ 100 R253P 1989 | 1989 | 4.11 | 9.61 | 5.50 |
| WZ 290 B418t 1983a | 1983 | 3.96 | 9.83 | 5.87 |
| WZ 350 R161t 1964 | 1964 | 5.16 | 8.21 | 3.05 |
| Y417 | 1977 | 5.48 | 9.44 | 3.96 |
| ZQU 55 A518 | 1976 | 5.60 | 9.77 | 4.17 |

# Footnotes

The Library of Congress considers paper testing in the range of 6.8-7.2 to be neutral.

The Library of Congress established this range at a time they were testing a variety of deacidification processes.  The lower number was chosen because they felt that if a book is improved from highly acidic to about neutral that is a successful treatment.  The upper number was chosen because their testing has indicated that there is no danger of damage due to high pH below that number.

Although the Library of Congress specifications call for a minimum of 1.5, they now consider 1.2 to acceptable and will be changing their specifications.